-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep21arlv.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Low Viscosity Epoxy Coating Features Acid Resistance

Master Bond EP21ARLV is a two part epoxy that may be used as an adhesive, sealant, coating or encapsulant. The product is capable of withstanding prolonged exposure to a wide range of chemicals, such as 70% sulfuric acid, 10% hydrochloric acid, 10% nitric acid and butyl acetate to name a few. Both parts A and B have a low viscosity of 3,000-6,000 cps and 4,000-6,000 cps, respectively. “With its low viscosity and acid resistance, EP21ARLV is a go-to material for potting and encapsulations in battery applications,” says Rohit Ramnath, Senior Product Engineer. “This combination is especially useful in applications where protection from acids is crucial.”

The mix ratio of EP21ARLV is 100 to 50 by weight, and it cures at room temperature. However, the addition of heat not only speeds up the curing process but it is also vital for optimizing acid resistance. It is a reliable electrical insulator with a volume resistivity greater than 1014 ohm-cm at 75°F, and dielectric strength of 440 volts/mil at 75°F, for a 1/8 inch test sample. Other noteworthy properties include a tensile strength of 8,000-9,000 psi, a Shore D hardness of 80-90 and a tensile modulus of 350,000-400,000 psi. It is serviceable over the temperature range of -60°F to +250°F.

This compound bonds well to a variety of substrates including metals, ceramics, composites and many plastics and rubbers. It is available for use in ½ pint, pint, quart and gallon container kits. Specialty packaging is also available in gun dispensers. The standard color of Part A is clear and Part B is amber clear, although it can be formulated in many different colors upon request. EP21ARLV does not contain solvents and is RoHS compliant.

Master Bond Chemically Resistant Epoxy Systems

Master Bond EP21ARLV is an acid resistant epoxy that features low viscosity, and electrical insulation. This versatile two component system can be used for high performance bonding, sealing, coating and encapsulating. Read more about Master Bond’s chemically resistant adhesives at https://www.masterbond.com/properties/chemical-resistance or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep29lpaoht

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #