The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep40tcmed.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, Electrically Insulative Epoxy for Medical Device Applications

Master Bond EP40TCMed is a two part, room temperature curing epoxy system that meets the requirements of ISO 10993-5 for non-cytotoxicity. It is thermally conductive, electrically non-conductive and can be utilized as an adhesive or sealant in various medical and wearable device applications.

This toughened epoxy delivers an elongation of 60-70%. It has good strength properties with a tensile lap shear strength between 2,300 and 2,500 psi, a T-peel strength of 40-60 pli and a low tensile modulus of 5,000-15,000 psi at room temperature, making it ideal for applications where low stress is needed. The system’s small particle size filler allows for effective heat transfer when applied in thin layers, lowering its thermal resistance. It is also capable of withstanding exposure to EtO, radiation and several sterilants, as well as anti-microbial cleaning agents. Serviceable from -100°F to +300°F [-73°C to +149°C], EP40TCMed features reliable electrical insulation characteristics with a dielectric constant of 4.4 at 60 Hz and a volume resistivity greater than 1015 ohm-cm. Its thermal conductivity is 8-11 BTU•in/(ft2•hr•°F) [1.16-1.60 W/(m•K)].

EP40TCMed offers convenient handling with a 1:1 mix ratio by weight, and has a relatively long working life of 2-3 hours for a 100 gram batch of mixed epoxy at 75°F. After mixing, the epoxy has a moderate viscosity of 80,000-100,000 cps, which is useful for applications where some, but not too much flow is required. Upon cure, it has low shrinkage and a hardness of 70-80 Shore D.  EP40TCMed comes in standard sized units of ounce jars, ½ pint, pint, quart, and gallon kits. It is also available in premixed and frozen syringes.

Master Bond Biocompatible Adhesives

Master Bond EP40TCMed is a thermally conductive, electrically insulative epoxy that meets ISO 10993-5 specifications. This two part, high strength, high elongation epoxy can resist exposure to various sterilization processes. Read about Master Bond medical grade adhesives at https://www.masterbond.com/properties/biocompatible-adhesives or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep40tcmed

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #