-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep40tc .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, Electrically Non-Conductive, Low Outgassing Epoxy

Master Bond EP40TC is a two part epoxy system, designed for bonding, sealing and encapsulating applications where thermal conductivity and electrical insulation are required. With a high thermal conductivity value of 8-11 BTU•in/(ft2 •hr•°F) [1.16-1.60 W/(m•K)], it is formulated with a small particle size filler making it ideal for filling small cavities and applying the product in thin sections. Its volume resistivity is greater than 1015 ohm-cm.

“EP40TC’s key distinguishing factor is that there is no compromise on the bond strength while providing excellent elongation and toughness. It has a high strength profile with a tensile lap shear strength of 2,300-2,500 psi, an elongation of 60-70%, and a tensile modulus of 5,000-15,000 psi,” says Rohit Ramnath, Senior Product Engineer. “Also, it meets NASA low outgassing specifications which is a prerequisite for many aerospace, electronic, and optical applications.”

Serviceable from -100°F to +300°F, this toughened system resists thermal cycling, vibration and shock. EP40TC exhibits a high peel strength of 40-60 pli and Shore D hardness of 70-80 at 75°F. It features a convenient 1:1 mix ratio, and cures in 2-3 days at room temperature or faster with the addition of heat. This compound adheres well to a variety of substrates such as metals, composites, glass, and many plastics. EP40TC is available in standard packaging, as well as premixed and frozen syringes.

Master Bond Thermally Conductive, Electrically Insulating Adhesives

Master Bond EP40TC is a two part epoxy system used for bonding, sealing and encapsulating. It meets NASA low outgassing requirements and is able to transfer heat without conducting electricity.  Read more about Master Bond’s electrically insulating adhesives at https://www.masterbond.com/properties/electrically-insulative-adhesive-systems  or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep40tc

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #