The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/led405med.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Biocompatible, Nanosilica Filled LED Curable Adhesive

Master Bond LED405Med is a one component, LED curing adhesive system that meets ISO 10993-5 cytotoxicity requirements for use in medical device assembly. “Since this system does not need a UV light for curing it is intrinsically more user friendly”, says Rohit Ramnath, Senior Product Engineer. “LED405Med has a nanosilica filler resulting in both lower shrinkage upon cure, as well as greater dimensional stability with a coefficient of thermal expansion of 35-40 in/in x 10-6/°C. This product cures to a hardness of 65-75 Shore D, indicating that it is not too stiff, thereby offering good toughness.”

LED405Med is optically clear, with a refractive index of 1.50, and offers excellent light transmission properties. This electrically insulative system features a high volume resistivity of more than 1014 ohm-cm and a low dielectric constant of 4.2 at 60 Hz. It has good flowability with a viscosity of 2,000-8,000 cps and can be used for bonding, sealing and coating. LED405Med cures up to 0.125 inch thick and is suitable for small encapsulations involving optical assemblies or other sensitive components.

This no-mix system cures fully tack-free upon exposure to a 405 nm wavelength light source without any oxygen inhibition.  In thinner sections, full cures can be achieved in 30-45 seconds. The rate of cure depends upon the intensity of the light source, the thickness of the adhesive layer and the distance from the light to the adhesive. LED405Med is serviceable from -60°F to +250°F and withstands gamma radiation as well as various chemical sterilants including EtO.

Master Bond LED Curing Adhesives

Master Bond LED405Med is a single component, LED curing adhesive, sealant, coating and encapsulating compound for medical device assembly. This nanosilica filled system offers high optical clarity, dimensional stability and electrical insulation properties.  Read more about Master Bond’s LED curing adhesives at https://www.masterbond.com/products/led-light-curable-adhesives or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/led405med

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

For a demonstration of how to cure an LED curable adhesive utilizing Master Bond LED405Med, please visit: https://youtu.be/SkBWar9dZ9s

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #