Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  This email was sent to (%email%)

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/newsrelease/ep3htsmed.

----------------------------------

FOR IMMEDIATE RELEASE

New Electrically Conductive, Silver Filled 
Adhesive/Sealant is USP Class VI Approved

HACKENSACK, NJ – January 12, 2012 – Developed for rigorous bonding and sealing in demanding manufacturing applications, Master Bond EP3HTSMED epoxy system features a rapid cure schedule and a tensile shear strength exceeding 1,000 psi. It is 100% reactive and fully meets USP Class VI requirements for medical applications.

This silver-filled epoxy adhesive/sealant has remarkable electrical conductivity with a volume resistivity less than 0.001 ohm cm. Serviceable over the wide temperature range of -60°F to 400°F, EP3HTSMED is resistant to severe thermal cycling and many chemicals including water, fuels, oil, and most organic solvents.

EP3HTSMED is a thixotropic paste and has a specific gravity of 2.90 at 77°F. It requires no mixing and needs only contact pressure during a simple heat cure of 20 to 40 minutes at 300°F or 40 to 90 minutes at 250°F. With minimal shrinkage during cure and a Shore D hardness of 60 to 80, EP3HTSMED bonds well to a variety of substrates including metals, glass, vulcanized rubbers, ceramics, and many plastics.

Silver in color, this one component adhesive is packaged in syringes or glass jars. EP3HTSMED has a shelf life of 6 months in a glass jar and a shelf life 3 months when stored in a syringe at room temperature.

Master Bond High Strength, Electrically Conductive Adhesives

Master Bond EP3HTSMED offers exceptional thermal and electrical conductivity while fully meeting USP Class VI requirements. This no mix epoxy adhesive has versatile, rapid cure schedules. Read more about Master Bond’s electrically conductive adhesives at  http://www.masterbond.com/properties/electrically-conductive-adhesive-systems or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #