This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=su33.

----------------------------------

FOR IMMEDIATE RELEASE

High Temperature Resistant, Toughened 
Structural Adhesive Cures at Room Temperature

HACKENSACK, NJ – January 18, 2011 – Formulated for structural applications in extreme environments with temperatures from -80°F to +425°F, Master Bond Supreme 33 has superior resistance to thermal cycling, thermal shock and impact. This toughened, two-component epoxy offers high structural bond strength to a wide variety of substrates including metals, glass, ceramics, wood, vulcanized rubbers and many plastics. Supreme 33 also resists chemicals including water, oil and many organic solvents.

Supreme 33 has a mix ratio of 100 to 70 by weight or 1 to 1 by volume. It cures conveniently at room temperature in 48 to 72 hours. For optimal performance, the suggested schedule is curing overnight at room temperature followed by 2 to 3 hours at 150 to 200°F. This 100% reactive epoxy does not contain any solvents or diluents, has exceptional dimensional stability and features very low shrinkage upon cure.

It produces high performance bonds boasting a shear strength over 2,500 psi, a tensile shear strength greater than 7,500 psi and a T-peel strength exceeding 15 pli. With a volume resistivity of 1014 ohm-cm, a dielectric strength over 400 volts/mil, and a dielectric constant of 3.8 at 75°F, Supreme 33 is an outstanding electrical insulator that is widely used in the electronic, electrical, aerospace and OEM industries.  Supreme 33 is also available in a non-drip version called Supreme 33ND.

Master Bond Toughened Adhesives

Master Bond Supreme 33 combines exceptional durability and toughness for high temperature resistance bonding and sealing applications. Read more about Master Bond’s toughened epoxies at http://www.masterbond.com/lp/tabs/tp_pp_flextoughened.html or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #